PRODUCT:	AF-021-40-FS-00	REV110117

PRODUCT DESCRIPTION:	1 inch thick polyether foam with flame shield facing

FOAM

| Physical Property | Description - Value | Tolerance | Test Standard |
| --- | --- | --- | --- |
| Material | Polyether Polyurethane Foam | NA | NA |
| Color | Charcoal | NA | NA |
| Density | 1.8 lb/cf | +- 0.18 | ASTM D3574 |
| Elongation | 140% | minimum | ASTM D3574 |
| Tensile Strength | 12.0 psi | minimum | ASTM D3574 |
| Tear Strength | 1.00 pli | minimum | ASTM D3574 |
| Compression Set @ 50%, 22 Hours | 5% typical |  | ASTM D3574 Test D |
| Pores per inch | 60-70 typical |  |  |
| Service Temperature | -40 0F – 250 0F |  |  |
| Thermal Conductivity | 0.27 BTU-in/(Hr-ft2-0F) typical | 0.01 |  |
| Flammability | MVSS302, UL-94 HF-1 |  |  |

FACING

| Physical Property | Description - Value | Tolerance |
| --- | --- | --- |
| Material | Proprietary fiber blend |  |
| Thickness | 0.020 inch | +/- 10% |
| Color | Black |  |
| Weight | 1.5 oz/sy | +/- 10% |
| Tensile Strength – MD | 113 oz/in |  |
| Tensile Strength – CD | 124 oz/in |  |
| Chemical Resistance | Resistant to moisture, UV, and gasoline |  |
| Flammability | Self-Extinguish to FMVSS-302 |  |
| Fire resistance | Resists direct flame for > 8 minutes |  |

AVAILABLE SIZES

| Roll | 54" X 100' |
| --- | --- |
| Sheet | As Specified |

ABSORPTION COEFFICIENT AND SAA to ISO 354

| Frequency | Sound Absorption Coefficient |
| --- | --- |
| 100 | 0.13 |
| 125 | 0.18 |
| 160 | 0.19 |
| 200 | 0.20 |
| 250 | 0.29 |
| 315 | 0.37 |
| 400 | 0.51 |
| 500 | 0.64 |
| 630 | 0.85 |
| 800 | 0.96 |
| 1000 | 1.07 |
| 1250 | 1.12 |
| 1600 | 1.11 |
| 2000 | 1.02 |
| 2500 | 0.94 |
| 3150 | 0.89 |
| 4000 | 0.85 |
| 5000 | 0.72 |
| SAA | 0.76 |

ABSORPTION COEFFICIENT AND SAA to ASTM E1050

| Frequency | Sound Absorption Coefficient |
| --- | --- |
| 100 | 0.04 |
| 125 | 0.05 |
| 160 | 0.06 |
| 200 | 0.07 |
| 250 | 0.09 |
| 315 | 0.14 |
| 400 | 0.21 |
| 500 | 0.30 |
| 630 | 0.37 |
| 800 | 0.51 |
| 1000 | 0.67 |
| 1250 | 0.79 |
| 1600 | 0.91 |
| 2000 | 0.99 |
| 2500 | 0.93 |
| 3150 | 0.80 |
| 4000 | 0.69 |
| 5000 | 0.74 |
| SAA | 0.50 |