## TECH LOCK ™ SYSTEM                        REV111617

PRODUCT DESCRIPTION:	Hook & loop attachment system for acoustic absorbers

TECH LOOP 1™ FABRIC

| Physical Property | Description - Value | Test Standard |
| --- | --- | --- |
| Material | Polyester |  |
| Type | Nonwoven fleece |  |
| Weight | 2.5 oz/sq. yd | ASTM D 3776-96 |
| Tensile Adhesion | 81.9 oz |  |
| Repositionability | 1 time |  |
| Temperature range | -30 0F to 220 0F | Intermittent to 2500F |

TECH LOOP 2™ FABRIC

| Physical Property | Description - Value | Test Standard |
| --- | --- | --- |
| Material | Polyamide |  |
| Type | Knit UBL |  |
| Weight | 2.36 oz/sq. yd | ASTM D 3776-96 |
| Tensile Adhesion | 142.5 oz |  |
| Repositionability | Up to 5 times |  |
| Temperature range | -30 0F to 220 0F | Intermittent to 2500F |

TECH TABS™

| Physical Property | Description - Value | Test Standard |
| --- | --- | --- |
| Material | Nylon |  |
| Type | Molded hooks |  |
| Pressure Sensitive Adhesive | .002” Acrylic |  |
| Temperature range | -30 0F to 220 0F | Intermittent to 2500F |

Compliance Features:

- US Patent Reg. No. 5,476,796

- Meets the Requirements of RoHS through June 2013 Revision of SVHC (Restriction of Hazardous Substances European Union Directive – 2002/95/EC)

- Compliant with European Union REACH (Registration, Evaluation and Authorization of Chemical Substances - EC1907/2006)

THE VALUES PRESENTED ARE TYPICAL AND ARE NOT INTENDED FOR SPECIFICATION PURPOSES.  This information is provided without warranty, representation, inducement or license of any kind.  INCLUDING BUT NOT LIMITED TO THE IMPLIED WARRANTIES OF MERCHANTABILITY AND FITNESS FOR A PARTICULAR USE OR PURPOSE, except that it is accurate to the best of Technicon Industries’ knowledge or obtained from sources believed by Technicon Industries to be accurate, and Technicon Industries does not assume any legal responsibility for the use or reliance upon same.  Customers are encouraged to conduct their own tests for suitability and conformance.