## PRODUCT:	VB-300-00-FS-FS                        REV010818

PRODUCT DESCRIPTION:	1lb/ft2 PVC barrier with FLAME SHIELD Fire resistant scrim on both sides

BARRIER

| Physical Property | Description - Value | Tolerance |
| --- | --- | --- |
| Material | Flexible PVC vinyl (polyvinylchloride) |  |
| Color | Charcoal gray |  |
| Weight | 1.0 lb/ft² | +/- 0.1 lb/ft² |
| Thickness | 0.09 inch | +/- 0.01 inch |
| Flammability | MVSS-302 |  |
| Service Temperature | -40oF to 220oF |  |
| Chemical Resistance | Excellent for most acids, mild alkalis, oils and grease |  |

FACING

| Physical Property | Description - Value | Tolerance |
| --- | --- | --- |
| Material | Proprietary fiber blend |  |
| Thickness | 0.020 inch | +/- 10% |
| Color | Black |  |
| Weight | 1.5 oz/sy | +/- 10% |
| Tensile Strength – MD | 113 oz/in |  |
| Tensile Strength – CD | 124 oz/in |  |
| Chemical Resistance | Resistant to moisture, UV, and gasoline |  |
| Flammability | Self-Extinguish to FMVSS-302 |  |
| Fire resistance | Resists direct flame for > 8 minutes |  |

ACOUSTICAL PROPERTIES

ASTM E90 and E413 on 1 lb/sf barrier only

| Frequency (Hz) | 125 | 250 | 500 | 1000 | 2000 | 4000 | STC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TL (dB) | 17 | 19 | 24 | 29 | 34 | 40 | 28 |

Compliance Features:

- Meets the Requirements of RoHS through June 2013 Revision of SVHC (Restriction of Hazardous Substances European Union Directive – 2002/95/EC)

- Compliant with European Union REACH (Registration, Evaluation and Authorization of Chemical Substances - EC1907/2006)

THE VALUES PRESENTED ARE TYPICAL AND ARE NOT INTENDED FOR SPECIFICATION PURPOSES.  This information is provided without warranty, representation, inducement or license of any kind.  INCLUDING BUT NOT LIMITED TO THE IMPLIED WARRANTIES OF MERCHANTABILITY AND FITNESS FOR A PARTICULAR USE OR PURPOSE, except that it is accurate to the best of Technicon Industries’ knowledge or obtained from sources believed by Technicon Industries to be accurate, and Technicon Industries does not assume any legal responsibility for the use or reliance upon same.  Customers are encouraged to conduct their own tests for suitability and conformance.